## 62-296.701 Portland Cement Plants.

(1) Applicability. The emission limitations set forth in Rule 62-296.701, F.A.C., shall apply to kilns and clinker coolers which are part of a Portland Cement Plant.

(2) Emission Limitations.

(a) Kilns – No owner or operator of a Portland Cement kiln shall cause, permit, or allow the emission of particulate matter in excess of 0.50 pounds per ton to the kiln (dry basis, excluding fuel), or visible emissions the density of which is greater than 20 percent opacity.

(b) Clinker coolers – No owner or operator of a Portland Cement clinker cooler shall cause, permit, or allow the emission of particulate matter in excess of 0.25 pounds per ton of feed to the kiln (dry basis, excluding fuel), or visible emissions the density of which is greater than 20 percent opacity.

(3) Alternate Emission Limitations.

(a) Applicability. The alternate emission limitations set forth in paragraph 62-296.701(3)(b), F.A.C., shall apply to the Portland Cement plants located in Hillsborough County south of State HIghway 60 in Tampa.

(b) Emission Limitations.

1. Clinker Kilns All Portland Cement plants shall not cause, permit, or allow the emission of particulate matter from Clinker Kilns in excess of 95 lbs./hr. as determined by EPA Method 5 nor in excess of 40 lbs./hr. as determined by EPA Method 17, or visible emissions the density of which is greater than 20 percent opacity as measured using a certified in-stack transmissometer. When method 17 is used the stack temperature shall not exceed 500 degrees Fahrenheit.

2. Clinker Coolers – All Portland Cement plants shall not cause, permit, or allow the emission of particulate matter from Clinker Coolers in excess of 45 lbs/hr as determined by EPA Method 5, or visible emissions the density of which is greater than 20 percent opacity as determined by EPA Method 9.

(4) Test Methods and Procedures. All emissions tests performed pursuant to the requirements of this rule shall comply with the following requirements.

(a) For emissions units subject to the visible emissions standard in subsection 62-296.701(2), F.A.C., the test method shall be EPA Method 9, as described at 40 C.F.R. Part 60, Appendix A-4, adopted and incorporated by reference at Rule 62-204.800, F.A.C.

(b) A transmissometer shall be used to determine the opacity of the visible emissions regulated by the standard in subseciton 62-296.701(3), F.A.C. The transmissometer shall be calibrated with the opacity of in accordance with 40 C.F.R. Part 60, Appendix B, and 40 C.F.R. 60.13, adopted and incorporated by reference at Rule 62-204.800, F.A.C.

(c) The test method for particulate emissions shall be EPA Method 5, as described at 40 C.F.R. Part 60, Appendix A-3, adopted and incorporated by reference at Rule 62-204.800, F.A.C. The minimum sample volume shall be 30 dry standard cubic feet.

(d) Test procedures shall meet all applicable requirements of Chapter 62-297, F.A.C.

Rulemaking Authority 403.061 FS. Law Implemented 403.021, 403.031, 403.061, 403.087 FS. History–Formerly 17-2.650(2)(c)1., Amended 6-29-93, Formerly 17-296.701, Amended 11-23-94, 1-1-96, 7-10-14.