25-12.027 Welder Qualification.

(1) No welder shall make any pipeline weld unless the welder has qualified in accordance with Section 3 of American Petroleum Institute Standard 1104, 17th edition, 1988, Section IX of the American Society of Mechanical Engineers Boiler and Pressure Vessel Code 1977, or Sections 1, 2 & 3 of Appendix C of the Code of Federal Regulations Part 192, as amended through December 27, 1989, within the preceding 15 months, but at least once each calendar year.

(2) No welder shall weld with a particular welding process unless the welder has engaged in welding with that process within the preceding six calendar months. A welder who has not engaged in welding with that process within the preceding six calendar months must requalify for that process as set forth in subsection (1) herein.

Specific Authority 368.05(2) FS. Law Implemented 368.03 FS. History–New 1-7-92.