## 25-12.027 Welder Qualification.

(1) No welder shall make any pipeline weld unless the welder has qualified in accordance with Section 3 of American Petroleum Institute Standard 1104, Welding of Pipelines and Related Facilities, 20th edition, October 2005 including Errata/Addendum July 2007 and Errata 2 (2008), or Appendix C of 49 C.F.R. 192 (2008), within the preceding 15 months, but at least once each calendar year.

(2) No welder shall weld with a particular welding process unless the welder has engaged in welding with that process within the preceding six calendar months. A welder who has not engaged in welding with that process within the preceding six calendar months must requalify for that process as set forth in subsection (1) herein.

Rulemaking Authority 350.127(2), 368.05(2) FS. Law Implemented 368.03 FS. History–New 1-7-92, Amended 12-15-09.